Agip

# MOTOR OIL HD

CCMC G4/D4**

API SF/CC

Single-grade engine oil for all gasoline and not charged diesel engines in passenger cars and light commercial vehicles. Suitable for exhaust systems with catalytic converter.

Characteristics (typical figures):

| Agip MOTOR OIL HD | Unit |  | 20W-30 | 30 | 40 |  | Test method |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Kin. Viscosity at 40°C | mm²/s |  | 106 | 132 | 107 |  | DIN 51 550 |
| at 100°C | mm²/s |  | 12,0 | 14,7 | 11,9 |  | ASTM D 445 |
| Viscosity index |  |  | 102 | 112 | 101 |  | DIN ISO 2909 |
| Density at 15°C | kg/m³ |  | 891 | 892 | 895 |  | ASTM D 1298 |
| Flashpoint o. C. | °C |  | 240 | 240 | 240 |  | ASTM D 92 |
| Pourpoint | °C |  | -24 | -24 | -21 |  | ASTM D 97 |

Properties and Performance:

Agip MOTOR OIL HD types are single-grade engine oils made of high quality, ageing resistant base oils that have high natural viscosity indexes. Detergent additives take care of clean pistons and ring grooves, prevent coking, pigmenting and sludge deposits and therefore maintain the full performance of the engine oil. Wear protection additives ensure optimum lubrication of all bearings, cylinder faces, cams and other friction points. The good corrosion protection prevents the attack of acidic combustion residues on all internal engine parts.

Agip MOTOR OIL HD types are compatible with all commonly used ring and flat sealings in the engine manufacturing. The miscibility with other brand engine oils that meet the national and international standards and specifications is ensured.

Applications:

Agip MOTOR OIL HD types are high-quality, catalytic converter suitable, single-grade engine oils for modern, efficient gasoline and suction diesel engines in vehicles and for stationary equipment.

The selection of the suitable SAE grade is made in accordance with the specifications of the engine manufacturer in reference to the ambient temperature.

Please observe the manufacturer’s specifications when selecting products.

| Specifications: |  |
| --- | --- |
| API SF/CC | FORD EU SSM-2C-9011 A |
| CCMC G4/D4 ** | FORD USA ESE-M2C-153 C |
| MIL-L-46152C | GENERAL MOTORS 6085 M |

** invalid standard since 01.01.97

Health instructions:				Follow the safety instructions (regulations)

Disposing according to the guidelines:	Waste disposal no. 13 02 05

Water hazardous class (WGK):		2	self-classification according to VwVwS