PASSION 2T RACING is a completely synthetic lubricant for very high-powered two-stroke motorcycles used in street and sport conditions. It is formulated from the best synthetic bases and a specific additive package to impart exceptional service performance.

The product is suitable for both premix and injection use. It can be employed with unleaded gasoline.

PROPERTIES AND PERFORMANCES

Its special formula ensures superior cleanliness of the pistons, of the ring area and the exhaust system to minimise power loss and preignition troubles.

Its superior and carefully selected synthetic base oils ensures very high antiwear performances and excellent thermo-oxidative stability.

CHARACTERISTICS

Viscosity at 100°C			mm2/s					20

Viscosity at   40°C			mm2/s					182

Viscosity Index  									130

Flash Point COC				°C					210

Mass density at15/15°C			kg/L					0.895

RECOMMENDATIONS

Shake well before proceeding to mixture preparation.

PD/CvO

E-PASSION Racing 2T may-’99.

AgipBenelux B.V.

P.O. Box9410 - 3007 AK Rotterdam

Tel: +31-10-2941555 - Fax:+31-010-4294594