PASSION 2T/SM is a modern premix/injector lubricant formulated with premium mineral basestocks for use in medium air- cooled or water- cooled two-stroke engines (scooters, mopeds). It is suitable for use in conjunction with both leaded and unleaded gasoline.

PROPERTIES AND PERFORMANCES

The self-mixing capacity of PASSION 2T/SM  ensures immediate formation of a homogeneous blend under all climatic conditions.

Its low ash content minimises combustion chamber deposits, spark-plug fouling and the blocking of exhaust ports and manifolds.

Its detergent properties minimise lacquer formation and carbon deposits thus preventing piston-ring stocking.

PASSION 2T/SM combats rust and corrosion in the engine resulting from attack by combustion moisture and acids.

CHARACTERISTICS

Colour									Red

Viscosity at 100°C			mm2/s				8.7

Viscosity at   40°C			mm2/s				62

Viscosity Index  								112

Pour Point				°C				-30

Flash Point COC				°C				130

Mass density at15/15°C			kg/L				0,882

SPECIFICATIONS

PASSION 2T/SM meets the requirements of the API TC specification.

PD/CvO

NL-PASSION 2T/SM-AUG-‘00

AgipBenelux B.V.

P.O. Box9410 - 3007 AK Rotterdam

Tel: +31-10-2941555 - Fax:+31-010-4294594