Agip

PRECIS HLP

DIN 51 524

HLP

Hydraulic oil based on mineral oil with agents against corrosion, oil ageing and wear.

Characteristics (typical figures):

| Agip PRECIS HLP | Unit |  | 32 | 46 | 68 | Test method |
| --- | --- | --- | --- | --- | --- | --- |
| Kin. Viscosity at 40°C | mm²/s |  | 32 | 46 | 68 | ASTM D 445 |
| Density at 15°C | kg/m3 |  | 870 | 872 | 884 | ASTM D 1298 |
| Flashpoint o. C. | °C |  | > 185 | > 195 | 240 | ASTM D 92 |
| Pourpoint | °C |  | -21 | -18 | -22 | ASTM D 97 |
| Designation |  |  | HLP 32 | HLP 46 | HLP 68 | DIN 51 524 T.2 |

Properties and performance:

Agip PRECIS HLP - grades guarantee a reliable operation of the hydraulic system also with variations of the ambient temperatures. The low Pourpoint ensures the immediate readiness of the system for operation at low ambient temperatures. These oils have an excellent wear protection and very good oxidation stability as well as excellent corrosion protection properties. The excellent water separation ability prevents formation of emulsion and the good air separation ability and antifoam behaviour cause a fast escape of air. The compatibility with common sealing material in hydraulic systems and common interior paint coats is guaranteed.

Application:

Agip PRECIS HLP - grades are hydraulic fluids for hydraulic transmission systems as well as for control devices for all operational conditions and highest working pressures. The oil viscosity has to be in accordance with the operating instructions.

These oils are especially suitable for the application in stationary hydraulic systems.

Please observe the manufacturer specifications when selecting products.

### Additional physical-technical data:

| Agip Precis HLP | Unit | 22 | 32 | 46 | 68 | Test method |
| --- | --- | --- | --- | --- | --- | --- |
| Neutral.-Number (s) | mgKOH/g | 0,9 | 0,9 | 0,95 | 0,5 | DIN 51 558T.1 |
| Sulphate ash | wt-% | 0,25 | 0,2 | 0,2 | 0,17 | DIN 51 575 |
| Ageing behaviour increase of the NZ after 1000 h at 95°C | mgKOH/g | < 2 | 2,0 | 2,0 | <2,0 | DIN 51 587 in connection with DIN 51 558 Part 1 |
| Corr. effect on copper max. | Corr. grade | 1-100 A3 (DIN 51759) | 2-100A3 | 2-100A3 | 1-125 A3 (DIN 51 759) | DIN EN ISO 2160 |
| Corr.- protection properties against steel max. | Corr. grade | 0 - A (DIN 51759) | 0 - A | 0 - A | 0 - B | DIN 51 585 |
| Foaming behaviour at 25°C 95°C 25°C after 95°C | ( ml | S1B-50/0 S2B-10/0 S3B-20/0 | 150/0 75/0 150/0 | 150/0 75/0 150/0 | S1B-30/0 S2B-50/0 S3B-30/0 | DIN 51 566 |
| FZG-Test A/8,3/90 load stage |  | 10 | Min. 11 | Min. 11 | 12 | DIN 51 354 Part 2 |
| Mech. test in the vane-cell pump Ring weight loss | ( mg | 60 mg | 120 | 120 | 50 | DIN 51 389 Part 2 |
| Vane weight loss | ( mg | 5 mg | 30 | 30 | 12 |  |
| Behaviour against sealing material SRE-NBR 1 accord. to 168h at 100°C 13.1 | rel. Vol. change max. % | +6 | 12 | 12 | +3 | DIN 53 538 Part 1 in connection with DIN 53 521 |
| Change of the SHORE-A-hardness | SH | -3 | -7 | -7 | -1,5 | DIN 53 505 |

# Health instructions:	Follow the safety instructions!

Disposing according to the guidelines:	Waste disposal no. 13 01 10

Water hazardous class (WGK): 		1	self-classification according to VwVwS