Agip

# RADULA

DIN 51 517 T.1

C

High quality machine oil based on mineral oil from selective raffinate with excellent lubrication properties.

Characteristics (typical figures):

| Agip RADULA | Unit | 15 | Test method |
| --- | --- | --- | --- |
| Kin. Viscosity at 40°C | mm²/s | 14,2 | ASTM D 445 |
| at 100°C | mm²/s | 3,3 |  |
| Viscosity index |  | 98 | DIN ISO 2909 |
| Density at 15°C | kg/m³ | 860 | ASTM D 1298 |
| Flashpoint o. C. | °C | 200 | ASTM D 92 |
| Pourpoint | °C | -21 | ASTM D 97 |
| Designation |  | C |  |
| ISO-VG-grade |  | 15 |  |

Properties and Performance:

Agip RADULA has a high purity level, a favourable natural viscosity-temperature-behaviour and very good cold flow properties. The high ageing stability and temperature load capacity guarantee a low tendency for the formation of coke residues (oil carbon) and deposits. Furthermore it has good water separation properties. The compatibility with all commonly used sealing materials in the machine construction and going internal varnishes is ensured.

Applications:

Agip RADULA has various application possibilities in the general machine lubrication: for splash and circular lubrication of sliding and roller bearings, mechanical transmissions, compressors, vans and vacuum pumps, also suitable for combustion engines, as long as they may be lubricated with unalloyed mineral oils.

In the low viscosity grades Agip RADULA is mainly suitable for the lubrication of fast running aggregates. Higher viscosities are preferred for heavier power units with increased working temperatures and low revolution per minute.

Please observe the manufacturer’s specifications when selecting products.

Additional physical-technical data:

| Agip RADULA | Unit | 10 | 15 | 32 | 46 | 68 | 100 | 150 | 220 | 320 | 460 | Test method |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Demulsifying capacity 54°C | min. | --- | 30 | 30 | 30 | 30 | 30 | --- | --- | --- | --- | DIN 51 599 |
| 82°C | min. | --- | --- | --- | --- | --- | --- | 60 | 60 | 60 | 60 |  |

Health instructions: 		Follow the safety instructions!

Disposing according to the guidelines 	Waste disposal no. 13 02 05

Water hazardous class (WGK): 			2	according to VwVwS