Agip

# ROTRA CT

## SAE 10W, 30, 50

CAT TO- 4

Special lubricant for transmissions and drives of Caterpillar machines.

Characteristics (typical figures):

| Agip ROTRA CT |  | SAE 10W | SAE 30 | SAE 50 | Test method |
| --- | --- | --- | --- | --- | --- |
| Viscosity at -15°C | cP | - | - | 10.000 |  |
| at 40°C | mm²/s | 33 | 94 |  | DIN 51 562 |
| at 100°C | mm²/s | 5,5 | 10,5 | 18 |  |
| Viscosity index |  | 102 | 101 | 100 | DIN ISO 2909 |
| Density at 15°C | kg/m³ | 886 | 889 | 905 | DIN 51 757 |
| Flash point o. C. | °C | 223 | 243 | 255 | DIN ISO 2592 |
| Pourpoint | °C | -32 | -27 | -15 | DIN ISO 3016 |

Properties and Performance:

Agip ROTRA CT has well-balanced additives especially to obtain a maximum life span of the friction linings in power shift gears and to prevent grating and vibration with wet brakes.

Agip ROTRA CT is compatible with all used materials in the transmission manufacturing.

Applications:

Agip ROTRA CT 10, CT 30 and CT 50 is recommended by Caterpillar for the lubrication of power shift gears, direct drive transmissions, end drives, differentials, winches/cranks, clutch discs, transmissions and axle bearings.

Agip ROTRA CT 10 and CT 30 are especially designed for the application in Caterpillar hydraulic systems, but it may also be used for the lubrication of power shift gears, direct drive transmissions, transmissions and axle bearings where SAE grade 10W or 30 is prescribed by Caterpillar.

CAT TO-4 oils should now be used for mechanical transmission that previously had the recommendation API CD/CAT TO-2.

Agip ROTRA CT can be recommended for the application at ambient temperatures of -30°C to +0°C (SAE 10W), -20°C to +25°C (SAE 30) respectively -10°C to +50°C (SAE 50).

All viscosities of Agip ROTRA CT can only be applied for components of the transmission, but not as engine oil.

Please observe the manufacturer’s specifications when selecting products.

| Specifications: |  |  |
| --- | --- | --- |
| API CF/CF-2* |  | KOMATSU* |
| CATERPILLAR TO-4 |  | KOMATSU DRESSER* |
| ALLISON C-4 |  | EATON* |
| ZF TE-ML-03C (nur SAE 30)* |  | DANA* |

* only for SAE 30 and 50

| Health instructions: | Follow the safety instructions! |
| --- | --- |

| European waste catalogue: | 13 02 05 |
| --- | --- |

| Water hazardous class ( WGK): | 2 | classified according to VwVwS |
| --- | --- | --- |