Agip ROTRA HY DB

SAE 80W

API GL-4

Gear oil for Daimler-Benz vehicles and working machines.

Characteristics (typical figures):

| Agip ROTRA HY DB |  | 80W | Test |
| --- | --- | --- | --- |
| Kin. Viscosity at -26°C | mPa.s | 130.000 | DIN 51 550 |
| at 40°C | mm²/s | 95 |  |
| at 100°C | mm²/s | 11,6 | ASTM D 445 |
| Viscosity Index |  | 100 | DIN ISO 2909 |
| Density at 15°C | kg/m³ | 900 | ASTM D 1298 |
| Flash point o. C. | °C | 215 | ASTM D 92 |
| Pourpoint | °C | -27 | ASTM D 97 |

Properties and Performance:

Agip ROTRA HY DB is produced of base oils that already have a good viscosity-temperature-behaviour. At low temperatures the lower inner friction causes next to a reduction of wear smaller performance losses and therefore minimizes the fuel consumption.

Agip ROTRA HY DB contains EP additives that, in connection with a favorable viscosity high temperature characteristic, make the formation of a pressure absorptive lubrication film possible. The lubrication film is also resistant to high surface pressures such as in high loaded variable-speed transmission and in hypoid axle drives. Anti-wear additives reduce the abrasion at bearings and gear teeth. The good oxidation stability at high temperatures and in presence of catalytic effecting components prevent inadmissible viscosity increase and sludge formation and ensure long oil dwell time.

Agip ROTRA HY DB is compatible with all materials used in the transmission manufacturing.

Applications:

Agip ROTRA HY DB is prescribed for manual transmission in Daimler-Benz-vehicles, but also applicable for hypoid axle drives under normal working conditions and with normal axle tramp. Also suitable for the use in worm gears, end drives and variable-speed transmission of agricultural machinery and earth movers.

Please observe the manufacturer’s specifications when selecting products.

| Specifications: |  |  |
| --- | --- | --- |
| API GL-4 | MB 235.1 | MAN 341 (level) |

Health instructions:	Follow the safety instructions!

European waste catalogue:			13 02 05 (Ref.: 2001/118/CE)

Water hazardous class (WGK): 	2	according to VwVwS